## Slide 1: Why Dirt Sticks
Barbara Kanegsberg
BFK Solutions LLC
(310)459-3614
barbara@bfksolutions.com
Surface Finishers Educational Association (SFEA)
February 12, 2015
Orange CA

## Slide 2: BFK Solutions Critical Cleaning Consultants, est. 1994
As the industry leaders, we provide
  Process improvement, not product sales
  Experience, expertise, common sense
  Industry involvement: JS3 (military), IPC, ASTM, ISO delegate, EPA, FDA
Barbara Kanegsberg, “The Cleaning Lady”
  Biochemist, clinical chemist, manufacturing process
Ed Kanegsberg, “The Rocket Scientist”
  Physicist, engineer, process evaluation
“Clean Source” eNewsletter
  Free
  Sign up!
Editors, 2 volume “Handbook for Critical Cleaning,” CRC Press, 2nd edition, 2011

## Slide 3: Always question authority - including BFK Solutions
We make the best effort to provide accurate, up-to-date information
Information, especially quantitative information, is obtained from reliable references
It’s always prudent to reconfirm all technical and regulatory information from the appropriate supplier or regulatory agency
  MSDS
  Technical data sheet
  Most recent requirement or regulation
This presentation contains private and copyrighted material. Not to be distributed without permission of BFK Solutions, LLC

## Slide 4: May I have your attention, please!

## Slide 5: Overview: Why Dirt Sticks
How cleaning works
Why dirt sticks
How to make dirt “unstick”
  Or keep if from sticking
Challenges, finding balance

## Slide 6: Cleaning
Cleaning in manufacturing?
  Floors
  Walls
  Windows
  Workbenches
  Cleanrooms
What about the product?
  Manufacturing, repair, rework, restoration

## Slide 8: Many (maybe most) manufactured objects need cleaning
Electronics assemblies
Aerospace hardware
Military weapons
Implantable medical devices
Paintings, sculpture
Computer hardware
Coffin corners
Analytical instruments
Mixing chambers, product contact
Optics
Automotive parts
Reflectors prior to vapor deposition
Molded plastic parts
Miniature components
Nano-components
Parts made with 3D printing (additive manufacturing)

## Slide 9: What’s a hard surface?
Metals
Plastic
Elastomers
Composites
Glass
3D printed objects
The surface may be below the surface
The entire product may be essentially all surface

## Slide 10: Fears about residue
We SEE THE RESIDUE Our customers detect residue
Our monitoring methods detect residue
Our monitoring methods DON’T detect residue (even worse)
We think we have residue - we’re not sure
The residue sticks – we can’t remove it

## Slide 11: Critical Cleaning
Soil
  Matter out of place
    E.g: burnt on lasagna on a casserole
Cleaning
  Removing soil
Critical cleaning - performance
  “Tipping point” cleaning
  Removing stuff from a product surface that doesn’t belong there
  Green cleaning – separate issue, critical cleaning ought to be green
Most manufactured products have to be cleaned to work

## Slide 12: Is it soil? …..

## Slide 13
…or is it dirt?

## Slide 14: Soils
Solder flux (rosin, organic acid, low residue)
Oils, greases
Metal working fluids
Lapping, polishing compounds compounds
Particles (metal fines, chips, skin flakes, polishing grit, 3D powder)
Acids
Water
Solvent
Product Assortment
Residual product/breakdown (in processing equipment)
Deposited cleaning agent residue (including flux residue)
Rust-preventative
Bacteria, mold, life-forms (alive or dead)
Sterilizing chemicals or processes

## Slide 16: Steps & Functions of Cleaning System: Think About Cleaning Agent and Cleaning Process Together
(1) Wash
  Deliver cleaning agent to surface
  Provide cleaning action to remove soil without damage to surface
  Remove soils from proximity of surface (i.e. leave a clean surface)
(2) Rinse
  Remove residual cleaning agent
  Continue cleaning process
  Vapor degreasing solvent – self-rinse
(3) Dry
  Remove water, adsorbed solvent
Separate, distinguishable operations
  Allocate $$$ and design time appropriately
Restore cleaning agent for subsequent operation (Optional, but often desirable)
All steps: avoid product damage

## Slide 17: Cleaning is a Process
Cleaning chemistry
Force
Temperature
  Rule of thumb
  10 degree Centigrade increase in temperature doubles reaction rate
Time
  Wash, rinse, dry
Cleaning process influences
  Worker safety, chemical emissions
  Why dirt sticks

## Slide 18: Cleaning factors interac – e.g. temperature and solvency
KB number
  Kauri-Butanol number
  Higher number - > more aggressive solvent
  Does not work for oxygenated solvents
    Water
    Ketones (eg. acetone)

## Slide 19: Higher boiling point may help with less aggressive solvents
Cleaning Agent | KB Number | Boiling Point deg C.
Methylene chloride | 136 | 40
Trans-1,2-dichloroethylene | 117 | 47
HCFC-225 | 31 | 54
HFE-7100 | 10 | 61
n-Propyl bromide (nPB) | 125 | 71
Trichloroethylene | 129 | 87
Perchloroethylene | 90 | 121
d-limonene (eg. Citrasolv) | 76 | 178
Stoddard Solvent | 33 | 188
Methyl soyate | 61 | 315

## Slide 20: Overview: Why Dirt Sticks
How cleaning works
Why dirt sticks
How to make dirt “unstick”
  Or keep it from sticking
Challenges, finding balance

## Slide 21: Sometimes, you just know you’ll have cleaning problems

## Slide 22: What makes soil difficult to remove?
Manufacturing processes can impede cleaning
  Soil
  Force
  Heat
  Time
Product shape and material
Changes in regulations
  Environmental, safety

## Slide 23: A balancing act
What helps remove soil?
What makes soil stick?
Forces
Cleaning chemistry
Temperature
Time
Forces
Soil chemistry and size
Temperature
Time
  Product shape and material
Changes in regulations
  Limits available options

## Slide 24: Balancing forces
What helps remove soil?
What makes soil stick?
Chemical force
  Polar/dispersion
Physical force
  Impingement
  Agitation
Must obtain access to surface with soil
Chemical force
  Polar/dispersion
Physical force
  drive particles into substrate (plastic, glass, metal)
    Cleaning/Drying/Polishing

## Slide 25: Balancing chemicals and soils
What helps remove soil?
What impedes removal?
Type of cleaning agent
  Aqueous/organic solvent
Solvency
Wetting/penetration
Rinsing
Drying
Type of cleaning agent
  Polar/non-polar
Chemical nature of soil
  Silicone
  proteins
Particle size
  Small particles adhere
Dried soils
Crevices/holes

## Slide 26: Balancing temperature
What helps remove soil?
What makes soil stick?
Higher temperatures
  More vigorous agitation
  Melting, vaporization
  Lower viscosity
Higher temperatures
  Caramelization
  Flash drying
  Baked on soils
  Substrate change

## Slide 28: Balancing time
What helps remove soil?
What helps soil stick?
More time  more cleaning
Prompt cleaning
More time  more damage
Latency (prior to cleaning)
  Longer soil adheres, the harder it adheres

## Slide 29: Dispersion forces
http://itl.chem.ufl.edu/2045/lectures/lec_g.html
Symmetric molecule induces dipole

## Slide 30: Van der Waal’s Equation

## Slide 31: Why do dried soils and small particles stick?

## Slide 32: Gecko feet
Geckos can adhere to a “smooth” dry surface
  No sticky fluids exuded
  Thousands/millions of tiny hairs (cilia); each hair has a tiny spatula foot
  Foot provides surface area (many molecules) for dispersive attraction
  Microscopic dimension allows foot to fit into small surface irregularities
Small particles are like gecko feet
Dried soils are like gecko feet

## Slide 33: What manufacturers need in cleaning solvent – actual request by presenter at major workshop
No ODP, No HAP
Low/no VOC, GWP
Not toxic to workers
Non-flammable
Non-halogenated
No formulation variability
Non-aqueous
Evaporates with no residue
Low cost
Use in current cleaning equipment
No employee retraining
Low to no capital costs
Does not damage part
No/low rinse
Rapid drying
Do a TERRIFIC JOB of cleaning

## Slide 34: Presenter’s request to cleaning agent suppliers: Think outside the box
Barb’s response:
You want them to think outside the periodic table of the elements

## Slide 35: Issues hampering new cleaning agent development
Technical constraints (physical/chemical)
  Think Outside the Box versus Outside the Periodic Table
Market fragmentation
  Miniaturization, tight spacing
  Diversity, materials of construction
Development costs
  Very high
  Cleaning a small market segment
Regulatory requirements
  Increasing difficulty for approval

## Slide 36: Issues hampering new chemical development
Political chemistry
  Negative lobbying by chemical companies against competition
  To manufacturers
  To governmental agencies
Corporate environmental policy
  Global
  Draconian
    Eg: No halogens allowed - Acetone is ok!

## Slide 37: Newer cleaning chemistries tend to be less aggressive
Avoiding air toxics
VOCs vs ODCs
  If it doesn’t impact the stratosphere, it impacts the troposphere
There are many lists of chemicals to avoid
  Geographical specificity
  Government sponsored
  Company policy constraints
Smaller companies, job shops
  May have few effective choices, may impact performance
  They may assume LARGER, FINAL FABRICATORS will do the major cleaning

## Slide 38: “Biofeedback” loops – California pressure

## Slide 39: Examples - biofeedback
Lubricants reformulated nationally to achieve lower VOC levels
  ILMA/SCAQMD collaboration
  Thermogravimetric analysis
  Net result: higher boiling points, more residue
Ozone Transport Commission Regional Model rules
  Degreasing model rule a “cut and paste” of SCAQMD regs
  Very low VOC content

## Slide 40: Manufacturing issues, biobased cleaners
Unestablished toxicity
Residue on product
Product stability
  Breakdown of esters
Batch to batch consistency
Flammability
High boiling point
VOC

## Slide 41: Overview: Why Dirt Sticks
How cleaning works
Why dirt sticks
How to make dirt “unstick”
  Or keep it from sticking in the first place
Challenges, finding balance

## Slide 42: Know your product – product configuration
Know the consequences of configuration
  Blind holes, helicoils, tight spacing
  Miniaturization
  Additive manufacturing
Redesign product – if possible

## Slide 43: Know your product – materials of construction
Materials compatibility problems of “delicate” materials limits aggressiveness of cleaning process
  Light metals (eg. Al, Be)
  Composites
  Plastics – batch to batch variability
High porosity materials
  Adsorb soils or solvents
Plan the cleaning process to avoid the problem

## Slide 44: Avoid the problem in the first place
New products – control the euphoria of your designers
Educate the designers
  Teach them about critical cleaning/surface quality
  Encourage (coerce) them to talk to the techs
  Require them to assemble, clean, and coat their own product!

## Slide 45: Understand the soils
What are the residues?
  Organic, inorganic, salts, biologics
  Thin film, particle, adsorbed gas
Switch to a less adherent soil if possible
The process modifies the soil, makes them tougher to remove
  “water-soluble” lubes, newer metalworking fluids
  “water-soluble” fluxes
Keep an eye out for regulatory changes

## Slide 46: Understand the cleaning process – cleaning chemicals
Know what the cleaning agent is
  Aqueous
  Solvent (organic)
Soils it dissolves well, soils it dissolves poorly
  Oils
  Greases
  Mixed soils
  Particles

## Slide 47: Clean the part right away
Clean immediately
Clean later? Usually more cleaning
  Temperature, time changes soils
Store parts in a cleanroom bag?
  Won’t help if the parts are dirty
Shipped parts – harder to clean
  More time, temperature excursions

## Slide 48: Manage the supply chain
Make cleaning process a collaborative decision
Specify cleaning in the contract
  Immediate cleaning
  Make sure suppliers use a cleaning process that works
Audit periodically
Cheap, generic suppliers – may cost more in the long run

## Slide 49: Are you part of the supply chain?
Understand how the parts you supply are used
  Where could leftover dirt be a problem?
Anticipate your customer’s problems with soils
Become the cleaning solution for your customers
Tactfully educate your customers

## Slide 50: Cleaning chemistries are not snake oil! (usually)

## Slide 51: Hansen parameters: Absolute numbers & balance influence solvency
Compound | Non-polar (dispersive) | Polar | Hydrogen bonding
Perchloroethylene | 19.0 | 6.5 | 2.9
n-propyl bromide | 16.0 | 6.5 | 4.7
HFC 43-10mee (Vertrel™) | 12.9 | 4.5 | 5.3
HFE 7100 (Novec™) | 13.7 | 2.3 | 1.3
Trans-1233zd (Solstice™) | 15.5 | 4.5 | 2.2
Water | 8.6 | 13.4 | 25.8
Isopropyl alcohol | 15.8 | 6.1 | 16.4
Acetone | 15.5 | 10.5 | 7.0

## Slide 52: Solvency parameters – like paint chips

## Slide 53: Select the cleaning process carefully
Is it really removing the soils?
Are adherent soils likely to increase in newer products?

## Slide 54: Example – great expectations
Final assembler
Cleaning glass
Cleaning assorted metals
  including aluminum

## Slide 55: Unrealistic Expectations
Wants to “improve” supply chain
More suppliers
Less costly suppliers
Expects to use two cleaning systems
  Metals
  Glass
Some problems
  Inconsistent soils
  Dry soils

## Slide 56: Are you seeing a increase in soils that stick? - Monitor & Re-evaluate
Be aware of changes
Monitor the process
  Cleaning agents
  Water quality
  Surface quality
  Residue
Be on the lookout for changes
  In soils
  In cleaning agent formulations or availability

## Slide 57: Overview: Why Dirt Sticks
How cleaning works
Why dirt sticks
How to make dirt “unstick”
  Or keep it from sticking
Challenges, finding balance

## Slide 58: Desirable, beneficial contamination
Surface cleaning may impart desirable changes
Stents – people lived because of contamination
  R. Baier
  Interaction, polishing compound, heat, metal
  Non-thrombogenic surface
Is the process leaving a desirable residue?
  Rust preventative
  Primer
  Strike

## Slide 59: More surface area - > more cleaning
Soil – inevitable in manufacturing
Harder to clean
  Large surface area
  “hidden” or inaccessible surface area
Surface area relative to mass is increasing
  Micro components
  Nano components
  Products produced via additive manufacturing

## Slide 60: Additive manufacturing-3D Printing
Allows designs of product or equipment with complex surfaces
  Intricate shapes
  Internal cavities
  Individualized (“one-off”) products
Fascinating cleaning challenges

## Slide 61: Additive (3D) Cleaning Challenges

## Slide 64: Example – 3D Challenge - Particles
People worry about particles
  Military & ISO specs
General rules
  The more you clean, the more particles you remove
  If you change cleaning agents, you remove different populations of particles
  Eventually, cleaning erodes the surface
Existing products - we meet the rules
Additive
  Complex surfaces
  we haven’t written the rules
Needed: pragmatic decision on allowable particle levels

## Slide 65: Additive Manufacturing- Soil that sticks
Raw material (powder) residue
Cleaning, rinsing and drying internal areas
  Unexpected residue
New, exciting alloys, alloy gradients
Surface prep & coating challenges
Medical devices
  Comments by FDA person, MD&M (Feb, 2015)
    Would like to adopt additive
    Sees cleaning, particles as major issues

## Slide 66: TANSTAAFL (“There ain’t no such thing as a free lunch”) Robert Heinlein, “The Moon is a Harsh Mistress”
Better solvency desired
  If it dissolves the soil, it MAY damage the product
  Everyone wants a universal solvent
    How would you store it?
Safety, low environmental impact desired
  If a cleaning agent dissolves the soil
    it can impact you
      Our products depend on organic chemicals (metalworking fluids)
      We’re made of organic chemicals
    It can impact the environment

## Slide 67
Is there a ‘perfectly safe’ chemical?
Let’s ask
Cosimo de’ Medici

## Slide 68: Where did the de Medici’s get their poisons?

## Slide 69
From the garden, perhaps …
Treat all chemicals responsibly

## Slide 70: Cleaning: A never-ending balancing act

## Slide 71: “TANSTAAFL” - Cleaning, Surface Finishing
Cleaner is better?
  We want cleaner surfaces
More cleaning, more problems
  High temperature, more adherent soils
  Surface damage (materials compatibility)
  May remove beneficial contamination

## Slide 72: It’s a matter of finding balance
Find the optimum process to remove the soil
  without harming the worker
  without harming the environment
  without harming their pocketbook
  Without harming the product itself

## Slide 73: Questions? (310-459-3614 barbara@bfksolutions.com)